RAINBOW CHEMICAL

Organic and Inorganic Pigments

ZHEJIANG RAINBOW CHEMICAL CO.,LTD.

ADD:XIAOSHAN ECONOMIC DEVELOPMENT ZONE,HANGZHOU,CHINA

CERTIFICATE OF ANALYSIS

STANDARD:NA/R1003                Date 2011.03.21

(PRODUCT NAME)           MILORY BLUE

(COLOUR INDEX NO.)           P.B.27

(BATCH NUMBER)                20110320

(QUANTITY)                    3000KGS

(STANDARD)   NA/QR1003:  Export Standard

(COLOUR)      BLUE         :(FORM)     POWDER

| Testing Items | Standard Scale | Testing Results |
| --- | --- | --- |
| Color Shade |  |  |
| Tinting Strength | 100±5 | 100 |
| Oil Absorption | ≤48 | 41.5 |
| Volatile Matter at 105 | ≤4.5 | 1.00 |
| Soluble Matter in Water | ≤3.5 | 1.25 |
| Finess 60 (目) | ≤5.0 | 2.50 |
| Chromatic Aberration | △E≤1.00 | 0.260 |
| Recommended Applicatnts |  |
|  | MAINLY TO BE USED IN PAINT AND PRINTING INKS ECT FOR COLOR |
| Remarks |  |
| Conclusion | PASS |

ZHEJIANG RAIBOW CHEMICAL CO.,LTD.

ADD:Nanyang Economic Development Zone,Xiaoshan,Hangzhou,China

Tel:0086-571-81854756 Fax:0086-571-89267595

E-Mail:yshpigment@hotmail.com

RAINBOW CHEMICAL

Organic and Inorganic Pigments

TECHNICAL DATA SHEET

| PRODUCT SPECIFICATION |
| --- |
| Product Name: | Milory Blue |
| Chemical Structure |  |
| Colour Index | Pigment Blue 27/77510 |
| Cas Rn: | 14038-43-8 |
| Physical Form | Blue Powder |
| TEST PROPERTY | SPECIFICATION |
| Color Strength Equivalent | 100±5% |
| ΔE, ΔL,Δa, Δb | ≤1,±1,±1,±1 |
| PHYSICAL DATA | SPECIFICATION |
| PH Value | 6.0-7.0 |
| Density(200C) [g/cm3] | 1.70-1.80 |
| Specific Surface [m2/g] | 15-40 |
| Oil Absorption [g/100g] | 40-60 |
| 1050C Volatile Matter | ≤1.0% |
| Water Soluble Matter | ≤1.0% |
| Mesh Residue [100mesh] | ≤5% |
| RESISTANCE TO SOLVENTS | SPECIFICATION |
| Water | 4 |
| White Spirit | 4 |
| Ethanol | 4 |
| Methethyl ketone | 3 |
| Ethyl acetate | 3 |
| Toluene | 4 |
| FASTNESSES | SPECIFICATION |
| Light | 6 |
| Weather | 4 |
| Acid | 4 |
| Alkali | 4 |
| FIELD OF APPLICATION | Paint and Coatings ect |

ZHEJIANG RAIBOW CHEMICAL CO.,LTD.

ADD:Nanyang Economic Development Zone,Xiaoshan,Hangzhou,China

Tel:0086-571-81854756 Fax:0086-571-89267595

E-Mail:yshpigment@hotmail.com